Excitonic effects on radial breathing mode intensity of single wall carbon nanotubes

(supporting online material, K. Sato et al., Chem. Phys. Lett. 497, 94 (2010))

Supplement 1: Calculated E22S and E11LM resonance Raman intensities of RBM using the dielectric constant κ = 2.

In the table below, the data are arranged in columns and categorized into metallic SWNTs, type-I semiconducting SWNTs, and type-II semiconducting SWNTs where , respectively. The RBM intensity data are listed, namely, E11M lower branch for metallic SWNTs, and E22S for both type-I and type-II semiconducting SWNTs. The diameter (dt) range in this table is from 0.6 to 1.6 nm.

Note: Double click and scroll down the above box to view the complete list as an excel spreadsheet. You can also copy and save it to a separate excel file.

If you need the already separate excel file of the above table, download it here: http://flex.phys.tohoku.ac.jp/eii/rbmint.xls